## Slide 1: “100 times stronger than steel”
www.msm.cam.ac.uk/phase-trans
Iron is the standard against which life and new materials are compared
Iron Lady
Stalin
Steely personality
Tough as steel
Strong as steel
Iron will
Iron hand in a velvet glove
Iron Man 3
Iron maiden

## Slide 2
September 2001
Quote from BBC journalist, talking about England 5 and Germany 1
“Eriksson has married the midfield of Liverpool and Man. United into a unit that has class and creativity and silk and steel”
April 2000
Quote from Russian Space and Aviation Agency, Alexei Karsnov
“I’m optimistic (MIR space station) ….. There could be problems .. with the atmosphere support .. but the steel is OK”

## Slide 3
Quote from a teacher to me, by email
“I have to teach about scientists at work. I am obviously going to talk about famous ones, but I will talk about you as well.”
Query by email
“Please save my life. We want to know the elastic modulus of bainite. It’s a microstructure in steels.”
1400 million tonnes of steel used per annum. Without song and dance.
So if there is something stronger than iron, should we take it seriously?

## Slide 4
500 MPa
3000 MPa
1500 MPa

## Slide 7
Li et al. 1993

## Slide 8: Design a new bearing steel

## Slide 9
It is nonsense to talk about the invention of a new material on the basis of just one property.
“there is much work between measuring a single attractive property in a single alloy to demonstrating credibility for a particular application”
Dan Miracle, Materials Science and Technology (2015)

## Slide 10
Brenner:1956
Single crystals of iron

## Slide 11: What is the maximum strength of iron?
remember this number

## Slide 12: Spider’s silk

## Slide 13: Spider’s silk
Tensile strength 700 MPa
Density 1.3 g cm-3
“Specific strength 6 times greater than steel of identical tensile strength”
Steel has a much greater specific strength than osmium at the same tensile strength (Os 22.6 g cm-3)

## Slide 14
Commercial alloy made by Kobe Steel

## Slide 16
1 Denier: weight in grams, of 9 km of fibre
50-10 Denier
Scifer is 9 Denier

## Slide 17: Spider’s silk
Tensile strength 700 MPa
Density 1.3 g cm-3
Specific strength 5.38 MPa g-1 cm3
“Specific strength 6 times greater than steel of identical tensile strength”
Tensile strength of Scifer 5500 MPa
Density 7.8 g cm-3
Specific strength 7.05 MPa g-1 cm3
Steel has a greater specific strength for same diameter as the silk

## Slide 18: Spider’s silk
700 MPa, 30% elongation gives “toughness” of 105 MJ m-3
Spider’s silk is therefore “tougher than steel”
Physics Education
43 (2008) 57

## Slide 19: Twinning induced plasticity
TWIP steel on similar calculation has a toughness of 500 MJ m-3

## Slide 21
Claimed strength of carbon nanotube is 130 GPa
Edwards, Acta Astronautica, 2000
Claimed modulus is 1.2 TPa
Terrones et al., Phil. Trans. Roy. Soc., 2004

## Slide 22: How is the strength of nanotube calculated?
By ignoring the empty space within the nanotube
Therefore strength of steel, which has 32% space unoccupied, is greater by 47% than reported since time zero
But let us ignore this

## Slide 23
36000 km
tethered space elevator
Arthur C. Clark (1979)

## Slide 24
geosynchronous orbit

## Slide 25
strength 130 GPa
modulus 1.2 TPa
 | J g-1 | m s-1
Dynamite | 4650 | 6000
Nanotube | 5420 | 21500

## Slide 26
data from Pan et al. 1999, Yu et al. 2000

## Slide 27: Entropy
P
P / 2

## Slide 28
Binary solution

## Slide 33
An equilibrium number of defects.
Strength of a nanotube rope 2 mm long is less than 2000 MPa

## Slide 34
Strength produced by deformation limits shape: wires, sheets...
Strength in small particles relies on perfection. Doomed as size increases.
Summary

## Slide 35
Morinobu Endo, 2004

## Slide 36
Lee et al. Science (2008)

## Slide 37: Intrinsic strength of Graphene (samples 2 µm2)

## Slide 38
University of Manchester web site

## Slide 39
April 2011: graphene 10 times stronger than steel (Univerisity of Techn. Sydney)
http://www.popsci.com/science/article/2011-04/new-graphene-material-paper-thin-and-ten-times-stronger-steel
April 2014: graphene about 100 times stronger than steel (Manchester University)
now claimed to be 200 times stronger
http://www.bbc.co.uk/news/science-environment-27113732
August 2015: graphene is 200 times stronger than structural steel (Columbia University)
http://news.bbc.co.uk/1/hi/programmes/click_online/9491789.stm

## Slide 40
The graphene monolayers used in the experiments are defect-free because they are so small, something that precludes the existence of flaws — a condition that cannot be satisfied in macroscopic materials.
The researchers measured the intrinsic strength of the material — that is the maximum stress that a pristine (or defect-free) material can withstand just before all the atoms in a given cross-section are pulled apart at the same time. This was found to be 42 N m–1 and represents the intrinsic strength of a defect-free sheet.
July 2008, Physics World
http://physicsworld.com/cws/article/news/2008/jul/17/graphene-has-record-breaking-strength

## Slide 41
Daily Mail

## Slide 43: “100 times stronger than steel”
www.msm.cam.ac.uk/phase-trans
Really? or are we simply lacking scholars?
and fooling the public?